## Slide 1: Frustrated Magnetism
Ashvin Vishwanath
UC Berkeley
Acknowledgements: Fa Wang (MIT), Frank Pollman (Dresden), Arun Paramekanti (Toronto), Roger Melko & Anton Burkov (Waterloo), Donna Sheng (Northridge), Leon Balents (KITP).

## Slide 2: Preview – Quantum Spin Liquids
Recent development: An electrical insulator, which conducts heat like a metal!
A triangular lattice magnet

## Slide 3: Magnetic Insulators
Mott Insulators – Coulomb repulsion localizes electrons to atomic sites. Only spin degree of freedom.
U
e-
t
Mott Insulator: U>t
Typically, oxides of transition metals (Fe, Co, Ni, Mn, Cu etc.)
U

## Slide 4: Magnetic Insulators
Only spin degree of freedom. Simplest quantum many body system!
Typically, spins order :
  Except in frustrated systems
Example: La2CuO4 (parent compound of cuprates)
S=1/2 square lattice anti-ferromagnet
e-
t
Opposite Spins gain by virtual hopping:
J≈t2/U; H = J S1•S2
.J ≈ 1,000Kelvin; t,U ≈10,000 Kelvin

## Slide 5: Geometric Frustration
Frustration ~ cannot optimize all energetic requirements simultaneously.
Triangular Lattice:
Kagome Lattice:
#of ground states= (N sites)
(Classical Spin)
Accidental degeneracy of classical ground states

## Slide 6: Geometric Frustration
Today, mainly Ising Spins (S=+1, -1)
Note, Heisenberg spins:
Triangular Lattice:
(now, unfrustrated – unique ground state, upto symmetries)
Kagome Lattice:
Frustrated ((spins on a triangle must sum to zero)
Pyrochlore Lattice:
Frustrated (spins on a tetrahedron must sum to zero)

## Slide 7: Geometrical Frustration in Ice
Residual Entropy of Ice (1936):
Third law of Thermodynamics: S0→0

## Slide 8: Geometrical Frustration in Ice Pauling’s Solution:
Structure:
Bernal Fowler Rules – 2 H near, 2 H far.
Oxygen
Hydrogen
Alternate H site
Idea: Hydrogens remain disordered giving entropy
Spin version: Spin ice (Ho2Ti2O7)
Ho

## Slide 9: Geometric Frustration & Relief
Outline
1. Frustration relief by residual interactions
  here - complex orders from lattice couplings in CuFeO2
2. Selection by quantum/thermal fluctuations
here – ‘supersolid’ order by disorder.
Classically degenerate
Complex orders - but defined by Landau order parameter.

## Slide 10: Geometric Frustration & Relief
Outline
3. Quantum spin liquids.
No Landau order parameter.
Alternate descriptions?
Depends on the spin liquid!
eg. Topological order OR
Gapless excitations unrelated to symmetry
Gauge theories emerge (Tomorrow)
Strong tunneling

## Slide 11: Frustration and Relief - Lattice coupling
Restoring force
Change in J
Tchernyshyov et al., Penc et al., Bergmann et al. for pyrochlore
Seen in Triangular lattice material CuFeO2
Optimal Configuration?
Z state
Zigzag stripes
Fa Wang and AV, PRL (08).

## Slide 12: Magnetization Plateaus and CuFeO2
h/J
c=0.15, Dz=0.01J
m
1
2
3
Z state
Good agreement with known phases of Triangular magnet CuFeO2.
Prediction for 1/3 plateau structure.
Spin-Phonon model:
Fa Wang and AV, PRL 2008

## Slide 13: Complex Phase Structure of Triangular Spin Phonon Model
Violations of “Gibbs Phase Rule” (4 phases meet at a point – due to frustration)
  E1 - E2= E2 - E3= 0 (requires 2 parameters)
  E4 - E3= E4 – E1= 0 (accidental degeneracy – frustration)
  Also, on Kagome
Spin-phonon Phase Diagram in a field
(numerical Monte Carlo – simulated annealing)

## Slide 14: XXZ Model on triangular lattice
Anderson and Fazekas (1973) [Resonating Valence Bond – spin liquid proposal]. Highly anisotropic triangular lattice antiferromagnet:
Project into Ising ground state manifold. Treat J as a perturbation.
Groundstates: Hardcore Dimers on the Honeycomb lattice (2 to 1 map)

## Slide 15: XXZ Model on triangular lattice
Anderson-Fazekas proposal: Ground state superposition of different dimer coverings (Resonanting Valence Bonds - RVB)
Quantum Dynamics from J term
J
Note, J>0 has a sign problem
Consider J<0, no sign problem! Solve for ground state.
Map J>0 to J<0 problem, in Hilbert space of Ising ground states.
Solve model for J<0; more naturally viewed as a boson model with hopping t=-2J

## Slide 16: Spin-Boson Mapping
Spin-boson mapping:
Repulsion
Quantum Fluctuation: Boson hopping
Bosons on the Triangular lattice:
t=0 highly frustrated
Physical Realization: Ultra-cold Dipolar Atoms in an optical lattice?

## Slide 17: Supersolid order on the triangular lattice
Case 2. If Jz >>t
Case 1. If t >>Jz
uniform superfluid
Melko, Paramekanti, Burkov, A.V., Sheng and Balents, PRL 06; Haiderian and Damle; Wessel and Troyer
Expect a solid. Charge order (m)
No sign problem – large system sizes can be studied with Quantum Monte Carlo

## Slide 18: Supersolid order on the triangular lattice
Case 2. If Jz >>t
Case 1. If t >>Jz
uniform superfluid
Jz/t
9
superfluid
lattice supersolid
(Quantum Monte Carlo)
AND superfluid (ρs)
high & low density
Charge order (m)
t=1/2

## Slide 19: Triangular Lattice bosons with Frustrated Hopping
However, in the limit Jz >>t , a unitary transformation exists – that reverses the sign. Only works in the space of Ising ground states (dimer states) – projector P.
+
XXZ antiferromagnet on the triangular lattice
Sign Problem – cannot use Quantum Monte Carlo.
Fa Wang, Frank Pollman, AV, PRL 09. & D. Sheng et al. PRB 09.

## Slide 20: Triangular Lattice XXZ Model at Jz>>J
Unitary transformation:
  Diagonal in Sz basis.
  Thermodynamics of +t and –t models identical
Only in the limit Jz >>t
(ground state sector of Ising antiferromagnet)

## Slide 21: Triangular Lattice bosons with Frustrated Hopping
Immediate Implications for +t
  Ground state also has same solid order (U diagonal in density/Sz basis) as -t
  Same superfluid density at +t as –t (free energy with vector potential: F[A] identical)
  Also a SuperSolid
Nature of Supersolid order: obtained using a variational wavefunction approach (A. Sen et al. PRL (08), for the unfrustrated case)
  Excellent energetics/correlations for unfrustrated case.
Correlation functions evaluated using Grassman techniques invented to solve 2D dimer stat-mech.

## Slide 22: Phase Diagram of the XXZ Antiferromagnet
Ordering pattern obtained near t/Jz=0. If we include t/Jz=-1/2 (Heisenberg point) with 120o order. Can be connected smoothly.
Anisotropic XXZ S=1/2 Heisenberg magnet is ordered – deformed 120o order. Not a spin liquid.
XXZ antiferromagnet

## Slide 23: Connection to Lattice Gauge Theories
Hardcore Dimer model (on bond ij)
On a bipartite lattice:
  Define a vector field e
Realized quantum electrodynamics on D=2 Lattice. Also called U(1) gauge theory.
Gauss Law

## Slide 24: Confinement and Spin Liquid Phase
Lattice gauge theories – two possible phases:
  Confined phase – electric fields frozen. (magnetic order)
  Coulomb phase (gapless photon excitation as in Maxwell’s electrodynamics) (Spin liquid)
Remarkable general result (A. Polyakov)
  In D=2, lattice electrodynamics (U(1) gauge theory), has only one phase – confined phase.
  Spin liquid very unlikely in Anderson-Fazekas model.

## Slide 25: Beating confinement
To obtain deconfinement
  Consider other gauge groups like Z2 (eg. non-bipartite dimer models)
  Go to D=3 [spin ice related models]
  Add other excitations. [deconfined critical points, critical spin liquids]
  References:
  J. Kogut, “Introduction to Lattice Gauge Theories and Spin Systems” RMP, Vol 51, 659 (1979).
  S. Sachdev, “Quantum phases and phase transitions of Mott insulators “, page 15-29 [mapping spin models to gauge theories]
  We will discuss each of these tomorrow